| Section 900 MORTH 2013 | Section 900 Approved by MORTH dt. 11.03.2025 | Comments/ Suggestions |
| --- | --- | --- |
| # 901. GENERAL - 901.1 All materials to be used, all methods to be adopted and all works to be performed shall be strictly in accordance with the requirements of these Specifications. The Contractor shall set up a field laboratory at locations approved by the Engineer and equip the same with adequate equipment and personnel in order to carry out Quality Control for works and all the required tests as per Specifications and/or as directed by the Engineer. The provision and maintenance of the laboratory shall be as per Clause 120 and/or as directed by the Engineer. The list of equipment and the facilities to be provided shall be got approved from the Engineer in advance. - 901.2 The Contractor’s laboratory shall be manned by a qualified Materials Engineer/Civil Engineer assisted by experienced technicians, and the set-up should be got approved by the Engineer. - 901.3 The Contractor shall carry out quality control tests on the materials and work to the frequency stipulated in subsequent paragraphs. In the absence of clear indications about method and or frequency of tests for any item, the instructions of the Engineer shall be followed. - 901.4 For satisfying himself about the quality of the materials and work, quality control tests will also be conducted by the Engineer (by himself, by his Quality Control Units or by any other agencies deemed fit by him), generally to the frequency set forth hereunder. Additional tests may also be conducted where, in the opinion of the Engineer, need for such tests exists. - 901.5 The Contractor shall provide necessary co-operation and assistance in obtaining the samples for tests and carrying out the field tests as required by the Engineer from time to time. This shall include provision of laboratory equipment, transport, consumables, personnel including labour attendants, assistants in packing and dispatching and any other assistance considered necessary in connection with the tests. - 901.6 For the work of embankment, subgrade and pavement, construction of subsequent layer of same or other material over the finished layer shall be done after obtaining permission from the Engineer. Similar permission from the Engineer shall be obtained in respect of all other items of works prior to proceeding with the next stage of construction. - 901.7 The Contractor shall carry out modifications in the procedure of work, if found necessary, as directed by the Engineer. Works falling short of quality shall be rectified/ redone by the Contractor at his own cost, and defective work shall also be removed from the site of works by the Contractor at his own cost. - 901.8 The cost of laboratory building including essential supplies like water, electricity, sanitary services and their maintenance and cost of all equipment, tools, materials, labour and incidentals to perform tests and other operations of quality control according to the Specification requirements shall be deemed to be incidental to the work and no payment shall be made for the same. If, however, there is a separate item in the Bill of Quantities for setting up of a laboratory and installing testing equipment, such work shall be paid for separately. - 901.9 For testing of soils/soil mixes, granular materials and mixes, bituminous materials and mixes, cement concrete materials and mixes, aggregates, cores etc., samples in the required quantity and form shall be supplied by the Contractor at his own cost. - 901.10 For cement, bitumen, steel, emulsion, road marking paint, sign boards, geo-synthetics and similar other materials where essential tests are to be carried out in the presence of Engineer at the manufacturer’s plants or at laboratories other than the site laboratory, the cost of samples, sampling, testing and furnishing of test certificates shall be borne by the Contractor. Manufacturer’s test certificate together with invoice or delivery challan shall be furnished for every lot of supply apart from tests to be conducted at site laboratory for prime properties of the material like cement, bitumen, etc. Where facilities for testing of materials are not available at site laboratory the same shall be tested at an outside laboratory in the presence of the Engineer. For specialized items such as sign boards, road marking paint, etc. the Engineer may order for third party test from an approved laboratory. - 901.11 The method of sampling and testing of materials shall be in accordance with the requirements of the relevant Indian Standards and these Specifications. Where they are contradicting, the provisions in these Specifications shall be followed. Where they are silent, sound engineering practices shall be adopted. The sampling and testing procedure to be used shall be as approved by the Engineer and his decision shall be final and binding on the Contractor. The cost of all tests shall be borne by the Contractor. - 901.12 The materials for embankment construction shall be got approved from the Engineer. The responsibility for arranging and obtaining the land for borrowing or exploitation in any other way shall rest with the Contractor who shall ensure smooth and uninterrupted supply of materials in the required quantity during the construction period. Similarly, the supply of aggregates and other materials for construction shall be from sources approved by the Engineer. Responsibility for arranging uninterrupted supply of materials from the source shall be that of the Contractor. - 901.13 Defective Materials All materials which the Engineer has determined as not conforming to the requirements of the Contract shall be rejected whether in place or not; they shall be removed immediately from the site as directed. Materials, which have been subsequently corrected, shall not be used in the work unless approval is accorded in writing by the Engineer. Upon failure of the Contractor to comply with any instruction of the Engineer, the Engineer shall have authority to cause the removal of rejected material and to deduct the removal cost thereof from any payments due to the Contractor. - 901.14 Imported Materials The Contractor shall furnish a list of materials/finished products manufactured, produced or fabricated outside India which he proposes to use in the work. The Contractor shall not be entitled to extension of time for acts or events occurring outside India and it shall be the Contractor’s responsibility to make timely delivery to the job site of all such materials obtained from outside India. The materials imported from outside India shall conform to the relevant Specifications of the Contract. In case where materials/finished products are not covered by the Specifications inthe Contract, the details of laboratories/establishments where tests are to be carried out shall be specifically brought out and agreed to in the Contract. The Contractor shall furnish to the Engineer a certificate of compliance of the tests carried out. In addition, certified mill test reports clearly identified in the lot of materials shall be furnished at the Contractor’s cost. # 902 CONTROL OF ALIGNMENT, LEVEL AND SURFACE REGULARITY - 902.1 General All works performed shall conform to the lines, grades, cross sections and dimensions shown on the drawings or as directed by the Engineer, subject to the permitted tolerances described herein-after. - 902.2 Horizontal Alignment Horizontal alignment shall be reckoned with respect to the centre line of the carriageway as shown on the drawings. The edges of the carriageway as constructed shall be correct within a tolerance of ± 10 mm therefrom. The corresponding tolerance for edges of the roadway and lower layers of pavement shall be ± 25 mm. - 902.3 Surface Levels The levels of the subgrade and different pavement courses as constructed, shall not vary from those calculated with reference to the longitudinal and cross-profile of the road shown on the drawings or as directed by the Engineer beyond the tolerances mentioned in Table 900-1. Table 900-1 : Tolerances in Surface Levels 1); Subgrade; ±20 mm. 2); Sub-base. (a) Flexible pavement; ±10 mm. (b) Concrete pavement; ±6 mm. 3); Base-course for flexible pavement. (a) Bituminous Base/Binder course; ±6 mm. (b) Granular. (i) Machine laid; ±10 mm. (ii) Manually laid; ±15 mm. 4); Wearing course for flexible pavement. (a) Machine laid; ±6 mm. (b) Manually laid; ±10 mm. 5); Cement concrete pavement; ±5 mm. Provided, however, that the negative tolerance for wearing course shall not be permitted in conjunction with the positive tolerance for base course, if the thickness of the former is thereby reduced by more than the following limits: - 4 mm for bituminous wearing course of thickness 40 mm or more - 3 mm for bituminous wearing course of thickness less than 40 mm - 5 mm for concrete pavement slab For checking compliance with the above requirement for subgrade, sub-base and base course, measurements of the surface levels shall be taken on a grid of points placed at 6.25 m longitudinally and 3.5 m transversely. For any 10 consecutive measurements taken longitudinally or transversely, not more than one measurement shall be permitted to exceed the tolerance as above, this one measurement being not in excess of 5 mm above the permitted tolerance. For checking the compliance with the above requirement for bituminous wearing courses and concrete pavements, measurements of the surface levels shall be taken on a grid of points spaced at 6.25 m along the length and at 0.5 m from the edges and at the centre of the pavement. In any length of pavement, compliance shall be deemed to be met for the final road surface, only if the tolerance given above is satisfied for any point on the surface. - 902.4 Surface Regularity of Pavement Courses The longitudinal profile shall be checked with a 3 metre long straight edge/moving straight- edge as directed by the Engineer at the middle of each traffic lane along a line parallel to the centre line of the road. The maximum permitted number of surface irregularities shall be as per Table 900-2. Table 900-2 : Maximum Permitted Number of Surface Irregularities Surfaces of Carriageways and Paved Shoulders; Surfaces of Laybys, Service Areas and all Bituminous Base Courses. Irregularity; 4 mm; 7 mm; 4 mm; 7 mm. Length (m); 300; 75; 300; 75; 300; 75; 300; 75. Number of Surface Irregularities on National Highways/ Expressways*; 15; 9; 2; 1; 40; 18; 4; 2. Number of Surface Irregularities on Roads of lower Category*; 40; 18; 4; 2; 60; 27; 6; 3. *Category of each section of road as described in the Contract. The maximum allowable difference between the road surface and underside of a 3 m straight-edge when placed parallel with, or at right angles to the centre line of the road at points decided by the Engineer shall be: for pavement surface (bituminous and cement concrete); 3 mm. for bituminous base courses; 6 mm. for granular sub-base/base courses; 8 mm. for sub-bases under concrete pavements; 10 mm. for subgrade; 15 mm. - 902.5 Rectification Where the surface regularity of subgrade and the various pavement courses fall outside the specified tolerances in Clause 902.4, the Contractor shall be liable to rectify these in the manner described below and to the satisfaction of the Engineer. i) Subgrade: Where the surface is high, it shall be trimmed and suitably compacted. Where the same is low, the deficiency shall be corrected by scarifying the lower layer and adding fresh material and recompacting to the required density. The degree of compaction and the type of material to be used shall conform to the requirements of Clause 305. ii) Granular Sub-base: Same as at (i) above, except that the degree of compaction and the type of material to be used shall conform to the requirements of Clause 401. iii) Lime/Cement Stabilized Soil Sub-base: For lime/cement treated materials where the surface is high, the same shall be suitably trimmed while taking care that the material below is not disturbed due to this operation. However, where the surface is low, the same shall be corrected as described herein below:. For cement treated material, when the time elapsed between detection of irregularity and the time of mixing of the material is less than 2 hours, the surface shall be scarified to a depth of 50 mm, supplemented with freshly mixed materials as necessary and recompacted as per the relevant specification. When this time is more than 2 hours, the full depth of the layer shall be removed from the pavement and replaced with fresh material to Specification. This shall also apply to lime treated material except that the time criterion shall be 3 hours instead of 2 hours. iv) Water Bound Macadam/Wet Mix Macadam Sub-base/Base: Where the surface is high or low, the top 75 mm shall be scarified, reshaped with added material as necessary and recompacted as per Clause 404 in the case of Water Bound Macadam and to Clause 406 in the case of Wet Mix Macadam. v) Bituminous Constructions: For bituminous construction other than wearing course, where the surface is low, the deficiency shall be corrected by adding fresh material over a suitable tack coat, if needed, and recompacting as per specifications. Where the surface is high, the extra thickness in the affected layer shall be removed and replaced with fresh material and compacted to Specifications. For wearing course, where the surface is high or low, the full depth of the layer shall be removed and replaced with fresh material and compacted to specifications. In all cases where the removal and replacement of a bituminous layer is involved, the area treated shall not be less than 5 m in length and not less than 3.5 m in width. vi) Dry Lean Concrete Sub-Base: The defective length of the course shall be removed to full depth and replaced with material conforming to Clause 601. The area treated shall be at least 3 m long, not less than 1 lane width and extend to the full depth. Before relaying the course, the disturbed subgrade or layer below shall be corrected by levelling, watering and compacting. vii) Cement Concrete Pavement: The defective areas having irregularity exceeding 3 mm but not greater than 6 mm when tested with a 3 metre long straight edge may be rectified by scrabbling or grinding using approved equipment. When required by the Engineer, areas which have been reduced in level by the above operation(s) shall be retextured in an approved manner either by cutting grooves (5 mm deep) or roughening the surface by hacking the surface. If high areas in excess 6 mm or low areas in excess of 3 mm occur, exceeding the permitted numbers and if the Contractor cannot rectify, the slabshall be demolished and reconstructed at the Contractor’s expense and in no case the area removed shall be less than the full width of the lane in which the irregularity occurs and full length of the slab. If deemed necessary by the Engineer, any section of the slab which deviates from the specified levels and tolerances shall be demolished and reconstructed at the Contractor’s cost. - 902.6 Riding Quality The riding quality of bituminous concrete wearing surface, as measured by a standard towed fifth wheel bump integrator, shall not be more than 2000 mm per km # 903 QUALITY CONTROL TESTS DURING CONSTRUCTION - 903.1 General The materials supplied and the works carried out by the Contractor shall conform to the specifications prescribed in the Clauses for the relevant items of work. For ensuring the requisite quality of construction, the materials and works shall be subjected to quality control tests, as described hereinafter. The testing frequencies set forth are the desirable minimum and the Engineer shall have the full authority to carry out additional tests as frequently as he may deem necessary, to satisfy himself that the materials and works comply with the appropriate specifications. However, the number of tests recommended in Tables 900-3 and 900-4 may be reduced at the discretion of the Engineer if it is felt that consistency in the quality of materials can still be maintained with the reduced number of tests. Test procedures for the various quality control tests are indicated in the respective Sections of these Specifications or for certain tests within this Section. Where no specific testing procedure is mentioned, the tests shall be carried out as per the prevalent accepted engineering practice to the directions of the Engineer. Table 900-3 : Control Tests and their Minimum Frequency for Sub-Bases and Bases (Excluding Bitumen Bound Bases) Sl. No.; Type of Construction; Test; Frequency (min.). 1.; Granular; i) Gradation; One test per 400 cu m. ii) Atterberg limits; One test per 400 cu m. iii) Moisture content prior to compaction; One test per 400 cu m. iv) Density of compacted layer; One test per 1000 sq m. v) Deleterious constituents; As required. vi) CBR; As required. 2.; Lime/Cement Stabilised Soil Sub-base; i) Quality of lime/ cement; One test for each consignment subject to a minimum of one test per 5 tonnes. ii) Lime/Cement content; Regularly, through procedural checks. iii) Degree of pulverization; Periodically as considered necessary. iv) CBR or Unconfined Compressive Strength test on a set of 3 specimens; As required. v) Moisture content prior to compaction; One set of two tests per 500 sq m. vi) Density of compacted layer; One set of two tests per 500 sq m. vii) Deleterious constituents; As required. 3.; Water Bound Macadam; i) Aggregate Impact Value; One test per 1000 cu m of aggregate. ii) Grading of aggregate; One test per 250 cu m. iii) Combined Flakiness and Elongation Indices; One test per 500 cu m of aggregate. iv) Atterberg limits of binding material; One test per 50 cu m of binding material. v) Atterberg limits of screenings; One test per 100 cu m of aggregate. 4.; Wet Mix Macadam; i) Aggregate Impact Value; One test per 1000 cu m of aggregate. ii) Grading of aggregate; One test per 200 cu m of aggregate. iii) Combined Flakiness and Elongation Indices; One test per 500 cu m of aggregate. iv) Atterberg limits of portion of aggregate passing 425 micron sieve; One test per 200 cu m of aggregate. v) Density of compacted layer; One set of three tests per 1000 sq m. Table 900-4 : Control Tests for Bituminous Works and their Minimum Frequency Sl. No.; Type of Construction; Test; Frequency (min.). 1.; Prime Coat/ Tack Coat/ Fog Spray; (i) Quality of binder; Number of samples per lot and tests as per IS:73, IS:217 and IS:8887 as applicable. (ii) Binder temperature for application; At regular close intervals. (iii) Rate of spread of Binder; Three tests per day. 2.; Seal Coat/Surface Dressing; (i) Quality of Binder; Same as mentioned under Serial No. 1. (ii) Aggregate Impact Value or Los Angeles Abrasion Value; One test per 200 cu m of each source and whenever there is change in the quality of aggregate. (iii) Combined Flakiness and Elongation Indices; One test per 100 cu m of aggregate for each source and whenever there is change in the quality of aggregate. (iv) Stripping value of aggregates (Immersion Tray Test); One test of each source and whenever there is change in the quality of aggregate. (v) Water absorption of aggregate; -do-. (vi) Water sensitivity of mix; -do-. (vii) Grading of aggregate; Two tests per day. (viii) Soundness (Magnesium Sulphate/ Sodium Sulphate); One test for each source and whenever there is change in the quality of aggregate. (ix) Polished stone value (not applicable for SAM/SAMI); -do-. (x) Temperature of binder in boiler, aggregate in dryer and mix at the time of laying and compaction; At regular intervals. (xi) Rate of spread of materials; Same as mentioned under Serial No. 1. (xii) Percentage of fractured faces (When gravel is used); One test per 100 cu m of aggregate. 3.; Open-graded Premix Surfacing/Close-graded Premix Surfacing; (i) Quality of binder; Same as mentioned under Serial No. 1. (ii) Aggregate Impact Value or Los Angeles Abrasion Value; Same as mentioned under Serial No. 2. (iii) Combined Flakiness and Elongation Indices; Same as mentioned under Serial No. 2. (iv) Stripping value; Same as mentioned under Serial No. 2. (v) Water absorption of aggregates; Same as mentioned under Serial No. 2. (vi) Water Sensitivity of mix; Same as mentioned under Serial No. 2. (vii) Grading of aggregates; Same as mentioned under Serial No. 2. (viii) Soundness(Magnesium Sulphate and Sodium Sulphate); Same as mentioned under Serial No. 2. (ix) Polished stone value; Same as mentioned under Serial No. 2. (x) Temperature of binder at application; At regular interval. (xi) Binder content; Two tests per day per plant. (xii) Percentage of fractured faces; Same as mentioned under Serial No. 2. 4.; Bituminous Macadam; (i) Quality of binder; Same as mentioned under Serial No. 1. (ii) Aggregate Impact Value or Los Angeles Abrasion Value; Same as mentioned under Serial No. 2. (iii) Combined Flakiness and Elongation Indices; One test per 350 cu m for each source. (iv) Stripping value; Same as mentioned under Serial No. 2. (v) Water absorption of aggregates; Same as mentioned under Serial No. 2. (vi) Water Sensitivity of mix; Same as mentioned under Serial No. 2. (vii) Grading of aggregates; Same as mentioned under Serial No. 2. (viii) Soundness (Magnesium Sulphate/ Sodium Sulphate); Same as mentioned under Serial No. 2. (ix) Percentage of fractured faces; Same as mentioned under Serial No. 2. (x) Binder content; Same as mentioned under Serial No. 3. (xi) Control of temperature of binder and aggregate for mix and of the mix at the time of laying and rolling; Same as mentioned under Serial No. 2. (xii) Density of Comp layer; One test per 700 sq m area. (xiii) Rate of spread of Mixed Material; At regular intervals. 5.; Dense Bituminous Macadam/Bituminous Concrete; (i) Quality of binder; Number of samples per lot and tests as per IS:73 or IRC:SP:53, IS:15462. (ii) Aggregate Impact Value/ Los Angeles Abrasion Value; One test per 350 cu m of aggregate for each source and whenever there is change in the quality of aggregate. (iii) Flakiness and Elongation Indices; One test per 350 cu m of aggregate for each source and whenever there is change in the quality of aggregate. (iv) Soundness test (Sodium or Magnesium Sulphate test); One test for each source and whenever there is change in the quality of aggregate. (v) Water absorption of aggregates; One test for each source and whenever there is change in the quality of aggregate. (vi) Sand equivalent test; One test for each source and whenever there is change in the quality of aggregate. (vii) Plasticity Index; One test for each source and whenever there is change in the quality of aggregate. (viii) Polished stone value; One test for each source and whenever there is change in the quality of aggregate. (ix) Percentage of fractured face; One test per 350 cu m of aggregate when crushed gravel is used. (x) Mix grading; One set for individual constituent and mixed aggregate from dryer for each 400 tonnes of mix subject to minimum of two tests per day per plant. (xi) Stability and voids analysis of mix including theoretical maximum specific of loose mix; Three tests for stability, flow value, density and void contents for each 400 tonnes of mix subject to minimum of two tests per day per plant. (xii) Moisture Susceptibility of mix (AASHTO T283); One test for each mix type whenever there is change in the quality or source of coarse or fine aggregate. (xiii) Temperature of binder in boiler, aggregate in dryer and mix at the time of laying and compaction; At regular intervals. (xiv) Binder content; One set for each 400 tonnes of mix subject to minimum of two tests per day per plant. (xv) Rate of spread of mix material; After every 5th truck load. (xvi) Density of Compacted layer; One test per 700 sq m area. 6.; Sand Asphalt Base course; (i) Quality of binder; Same as mentioned under Serial No. 2. (ii) Aggregate Impact Value or Los Angeles Abrasion Value; Same as mentioned under Serial No. 2. (iii) Sand equivalent test; Same as mentioned under Serial No. 2. (iv) Plasticity Index; Same as mentioned under Serial No. 5. (v) Mix grading & binder content; Same as mentioned under Serial Nos. 2 and 3. (vi) Stability of Mix; Same as mentioned under Serial No. 5. (vii) Control of temperature of binder in boiler, aggregate in the dryer and mix at the time of laying and rolling; Same as mentioned under Serial No. 2. (viii) Thickness of layer; Same as mentioned under Serial No. 5. (ix) Density of Compacted layer; Same as mentioned under Serial No. 5. 7.; Slurry Seal and Micro surfacing; (i) Quality of Aggregate Sand Equivalent Value Water Absorption Soundness Test (Sodium/ Magnesium Sulphate Test); One per source/ site. (ii) Quality of Emulsion; One per lot of 20 t as per IS:8887. (iii) Aggregate Moisture; Two per day. (iv) Aggregate Gradation; Two per day at site. (v) Binder Content; Two per lane per Km. (vi) Calibration of Machine; Once per Project. (vii) Quantity of Slurry (By weight of aggregate); Daily (Travel time of Machine). 8.; Stone Matrix Asphalt; (i) Quality of binder; Number of samples per lot and tests as per IS:73 or IRC:SP 53, IS:15462. (ii) Aggregate Impact Value/ Los Angeles Abrasion Value; One test per 100 cu m of aggregate. (iii) Flakiness and Elongation Indices; One test per 100 cu m of aggregate. (iv) Soundness Test (Sodium and Magnesium Sulphate Test); One test for each method for each source and whenever there is change in the quality of aggregate. (v) Water absorption of aggregate; One test for each source and whenever there is change in the quality of aggregate. (vi) Sand equivalent test; One test for each source. (vii) Plasticity Index; One test for each source. (viii) Polished stone value; One test for each source. (ix) Percent of fractured faces; One test per 50 cu m of aggregate when crushed gravel is used. (x) Mix grading; One set for individual constituent and mixed aggregate from dryer for each 400 tonnes of mix subject to minimum of two tests per day per plant. (xi) Air voids and VMA analysis of mix including theoretical maximum specific gravity of loose mix; Three tests per day. (xii) Moisture Susceptibility of mix (AASHTO T 283); One test for each mix type whenever there is change in the quality or source of coarse or fine aggregate. (xiii) Temperature of binder in boiler, aggregate in dryer and mix at the time of laying and compaction; At regular intervals. (xiv) Binder content; One set for each 400 tonnes of mix subject to minimum of two tests per day per plant. (xv) Rate of spread of mix material; After every 5th truck load. (xvi) Density of compacted layer; One test per 250 sq m area. 9.; Mastic asphalt; (i) Quality of binder; Same as mentioned under Serial No. 5. (ii) Aggregate Impact Value and Los Angeles Abrasion Value; Same as mentioned under Serial No. 5. (iii) Combined Flakiness and Elongation Indices; Same as mentioned under Serial No. 5. (iv) Stripping value; Same as mentioned under Serial No. 2. (v) Water Sensitivity of mix; Same as mentioned under Serial No. 5. (vi) Grading of aggregates; Two tests per day per plant on the individual constituent and mixed aggregates from the dryer. (vii) Water absorption of aggregates; Same as mentioned under Serial No. 5. (viii) Soundness (Magnesium Sulphate/ Sodium Sulphate); Same as mentioned under Serial No. 5. (ix) Percentage of fractured faces; Same as mentioned under Serial No. 5. (x) Binder content and aggregate grading; Same as mentioned under Serial No. 3. (xi) Control of temperature of binder and aggregate for mixing and of the mix at the time of laying and rolling; At regular close intervals. (xii) Rate of Spread of Mixed Material; Regular control through check of layer thickness. (xiii) Hardness number; Minimum two tests per day. 10.; Recycled Material Grading of aggregate; Two tests per day. 11.; Cold Mixes; All tests as per S. No. 5. 12.; Quality of Modified Binder; Number of samples per lot and tests as per IS:15462.. 13.; Geotextiles; The requirements of Section 700 shall apply. Note: Daily, weekly, monthly reports on test results shall be prepared indicating the location of sampling and testing, deviation from the specified values for materials and works and remedial action taken in respect of removal of defective work shall certified be prepared by the Contractor. The test record shall be certified by the Engineer that these tests were done in his presence and testing carried as per prescribed methodology. - 903.2 Tests on Earthwork for Embankment, Subgrade Construction and Cut Formation - 903.2.1 Borrow Material ### Grid the borrow area at 25 m c/c (or closer, if the variability is high) to full depth of proposed working. These pits should be logged and plotted for proper identification of suitable sources of material. The following tests on representative samples shall be carried out for every 3000 cum for each source: a) Sand Content [IS:2720 (Part-4)]: 2 tests per 3000 cu m of soil. b) Plasticity Test [IS:2720 (Part-5)]: Each type to be tested, 2 tests. c) Density Test [IS:2720 (Part-8)]: Each soil type to be tested, 2 tests. d) Deleterious Content Test [IS:2720 (Part-27)]: As and when required by the Engineer. e) Moisture Content Test [IS:2720 (Part-2)]: Two tests. f) CBR Test on materials to be incorporated in the subgrade on soaked/unsoaked samples [IS:2720 (Part-16)] : One CBR test (average of three specimens) or closer as and when required by the Engineer. - 903.2.2 Compaction Control ### Control shall be exercised on each layer by taking at least one set of ten measurements of density for each 3000 sq m of compacted area, or closer as required to yield the minimum number tests results for evaluating a day’s work on statistical basis. The determination of density shall be in accordance with IS: 2720 (Part-28). Test locations shall be chosen only through random sampling techniques. If non-destructive tests are carried out, the number of tests shall be doubled. If considerable variations are observed between individual density results, the minimum number of tests in one set of measurement shall be increased. The acceptance criteria shall be subject to the condition that the mean density is not less than the specified density plus: However, for earthwork in shoulders (earthen) and in the subgrade, at least one set of ten density measurements shall be taken for every 2000 sq. m for the compacted area. In other respects, the control shall be similar to that described earlier. - 903.2.3 Cut Formation ### Tests for the density requirements of cut formation shall be carried out in accordance with Clause 903.2.2. - 903.3 Tests on Sub-bases and Bases (excluding Bitumen Bound Bases) The tests and their frequencies for the different types of bases and sub-bases shall be given in Table 900-3. The evaluation of density results and acceptance criteria for compaction control shall be on lines similar to those set out in Clause 903.2.2. - 903.3.1 Acceptance Criteria ### the acceptance criteria for tests on the strength of cement/lime stabilized soil and distribution of stabilizer content shall be subject to the condition that the mean value is not less than the specified value plus: - 903.4 Tests on Bituminous Construction - 903.4.1 Tests and Frequency ### The tests and their minimum frequencies for the different types of bituminous works shall be as given in Table 900-4. The Engineer may direct additional testing as required. - 903.4.2 Acceptance Criteria ### The acceptance criteria for tests on density shall be subject to the condition that the mean value is not less than the specified value plus: - 903.4.3 Where the Contract specifies the surface roughness requirements, in terms of Bump Integrator value, the surface roughness shall be measured by a calibrated Bump Integrator as per the procedure described in IRC:SP:16. The measurements shall be taken at centre line of each lane for a minimum completed length of one Km. - 903.5 Quality Control Tests for Concrete Road Construction - 903.5.1 Dry Lean Concrete Sub-base : - 903.5.1.1 Sampling and Testing of Cubes #### Samples of dry lean concrete for making cubes shall be taken from the uncompacted material from different locations immediately before compaction at the rate of 3 samples for each 1000 sq m or part thereof laid each day. The sampling of mix shall be done from the paving site. Test cubes of 150 mm size shall be made immediately from each mix sample. Cubes shall be made in accordance with the methods described in IS:516 except that the cubes shall be compacted by means of a vibratory hammer with the moulds placed on a level and rigid base. The vibrating hammer shall be electric or pneumatic type fitted with a square or rectangular foot having an area of between 7500 to 14000 sq.mm. The compaction shall be uniformly applied for 60± 5 seconds with a downward force of between 300 N and 400 N on to each of the three layers of the lean concrete material placed into the mould. The surface of each compacted layer shall be scarified before the next layer is added to give key for the next layer. The final layer shall be finished flush with the top of the cube mould. The dry lean concrete shall be cured in accordance with IRC :SP:49/IS:516. - 903.5.1.2 In-situ Density #### The dry density of the laid material shall be determined from three density holes at locations equally spaced along a diagonal that bisects each 2000 sq m or part thereof laid each day and shall comply with the requirements as per Clause 601.6.5.1. This rate of testing may be increased at the discretion of the Engineer in case of doubt or to determine the extent of defective area in the event of non-compliance. Density holes at random may be made to check the density at edges. - 903.5.1.3 Thickness #### The average thickness of the subbase layer as computed by the level data of sub-base and subgrade or lower sub-base shall be as per the thickness specified in the contract drawings. The thickness at any single location shall not be 8 mm less than the specified thickness. Such areas shall be corrected as stated in Clause 601.6.5.5. Areas which cannot be repaired should be replaced over full width. The extent of deficient area should be decided based on cores. - 903.5.1.4 Frequency of Quality Control Tests #### The frequency of quality control tests for levels, alignment and materials shall be as given in Table 900-6. - 903.5.2 Pavement Concrete - 903.5.2.1 Sampling and Testing of Beam and Cube Specimens #### At least three beams and three cube specimens, one set of three each for 7 day and 28 day strength tests shall be cast for every 150 cu m (or part thereof) of concrete placed during construction. On each day’s work, not less than three pairs of beams and cubes shall be made for each type of mix from the concrete delivered to the paving plant. Each pair shall be from a different delivery of concrete and tested at a place to be designated by the Engineer in accordance with the testing procedure as outlined in Clause 602.3.3. Groups of four consecutive results from single specimens tested at 28 days shall be used for assessing the strength for compliance with the strength requirements. The specimens shall be transported in an approved manner to prevent sudden impact causing fractures or damage to the specimen. The flexural strength test results shall prevail over compressive strength tests for compliance. #### 903.5.2.2 A quality control chart indicating the strength values of individual specimens shall be maintained for continuous quality assurance. Where the requirements are not met with, or where the quality of the concrete or its compaction is suspect, the actual strength of the concrete in the slab shall be ascertained by carrying out tests on cores cut at the rate of 2 cores for every 150 cu m. of concrete. The average of the results of crushing strength tests on these cores shall not be less than 0.8 x 0.85 times the corresponding characteristic compressive strength of cubes, where the height to diameter ratio of the cores is two. Where height to diameter ratio is not two, necessary corrections shall be made in calculating the crushing strength of cubes in the following manner.: The crushing strengths of cylinders with height to diameter ratios between 1 and 2 may be corrected to correspond to a standard cylinder of height to diameter ratio of 2 by multiplying with the correction factor obtained from the following equation: f = 0.11 n+0.78 where f = correction factor and n = height to diameter ratio The corrected test results shall be analysed for conformity with the specification requirements for cube samples. Where the core tests are satisfactory, they shall have precedence for assessing concrete quality over the results of moulded specimens. The diameter of cores shall not be less than 150 mm. If, however, the tests on cores also confirm that the concrete is not satisfying the strength requirements, then the concrete corresponding to the area from which the cores were cut should be replaced, i.e., at least over an area extending between two transverse joints where the defects could be isolated or over larger area, if necessary, as assessed by additional cores and their test results. The equivalent flexural strength at 28 days shall be estimated in accordance with Clause 602.3.3.2. In order to ensure that the specified minimum strength at 28 days is attained in 1 in 20 of all test beams, the mix shall be proportioned to give an average strength at 28 days exceeding the specified strength by 1.65 times the standard deviation calculated first from the flexural strengths of test beams made from the trial mix and subsequently from the accumulating result of flexural strengths of job control test beams. The standard deviation shall be re-calculated from the test results obtained after any change in the source or quality of materials and the mix shall be adjusted as necessary to comply with the requirements. An individual 28 day test strength below the specified strength shall not be evidence for condemnation of the concrete concerned if the average 28 day strength of this beam plus the preceding 5 and succeeding 4 beams exceeds the specified strength by 1.65 times the standard deviation and provided that there is no other evidence that the concrete mix concerned is substandard. Beams shall be made each day in pairs at intervals, each pair being from a different batch of concrete. At the start of the work, and until such time as the Engineer may order a reduction in the number of beams required, at least six pairs of beams and cubes shall be made each day, one of each pair for testing at 28 days for determination of minimum permissible flexural strength and the other for testing at an early age for the Engineer to assess the quality of the mix. When the first thirty number of 28-day results are available, and for so long as the Engineer is satisfied with the quality of the mix, he may reduce the number of beams and cubes required. During the course of construction, when the source of any material is to be changed, or if there is any variation in the quality of the materials furnished, additional tests and necessary adjustments in the mix shall be made as required to obtain the specified strength. The flexural strengths obtained on beams tested before 28 days shall be used in conjunction with a correlation between them and the 28 day flexural strengths to detect any deterioration in the quality of the concrete being produced. Any such deterioration shall be remedied without awaiting the 28 day strengths but the earlier strengths shall not constitute sole evidence of non-compliance of the concrete from which they were taken. Concrete shall be deemed not to comply with the Specification when more than one test beam in a batch has a 28 day strength less than the specified strength and the average 28 day flexural strength of the batch of beams is less than the specified strength plus 1.65 times the standard deviation of the batch. Should the concrete fail to comply with the Specification for strength as described above, the Contractor may, all at his own expense, elect to cut cores from the suspect concrete as the Engineer shall direct. From the relation between cube strength and flexural strength, the core strength shall be converted to flexural strength. The equivalent flexural strength at 28 days shall be the estimated in-situ strength multiplied by 100 and divided by the age-strength relation obtained from Table 900-5. Any concrete that fails to meet the strength specification shall be removed and replaced at Contractor’s expense. Table 900-5 : Age-Strength Relation of Concrete (Related to 100 per cent at 28 Days) Days; 0; 2; 4; 6; 8. 0; –; 41.0; 60.0; 71.0; 77.5. 10; 81.5; 85.0; 87.5; 90.0; 92.0. 20; 94.0; 96.0; 97.5; 98.5; 100.0. 30; 101.0; 102.0; 103.5; 104.5; 105.5. 40; 106.5; 107.0; 108.0; 109.5; 110.0. 50; 110.5; 111.0; 112.0; 112.5; 113.0. 60; 114.0; 114.5; 115.0; 115.5; 116.0. 70; 116.5; 117.0; 117.5; 118.0; 118.5. 80; 119.0; 119.5; 119.5; 120.0; 120.5. 90; 121.0; 121.5; 122.0; 122.0; 122.5. 100; 123.5; 123.5; 123.5; 124.0; 124.5. 110; 125.0; 125.0; 125.5; 125.5; 126.0. 120; 126.0; 126.0; 127.0; 127.0; 127.5. 130; 127.5; 128.0; 128.5; 128.5; 129.0. 140; 129.0; 129.5; 129.5; 130.0; 130.0. 150; 130.5; 130.5; 131.0; 131.0; 131.5. 160; 131.5; 131.5; 132.0; 132.0; 132.5. 170; 132.5; 132.5; 133.0; 133.0; 133.5. 180; 133.5; 134.0; 134.0; 134.5; 134.5. 190; 135.0; 135.0; 135.0; 135.5; 135.5. 200; 135.5; 135.5; 136.0; 136.0; 136.5. 210; 136.5; 136.5; 137.0; 137.0; 137.0. 220; 137.0; 137.5; 137.5; 137.5; 138.0. 230; 138.0; 138.5; 138.5; 138.5; 138.5. 240; 139.0; 139.0; 139.0; 139.5; 139.5. 250; 139.5; 140.0; 140.0; 140.0; 140.0. 260; 140.5; 140.5; 140.5; 140.5; 141.0. 270; 141.0; 141.0; 141.5; 141.5; 141.5. 280; 142.0; 142.0; 142.0; 142.0; 142.0. 290; 142.5; 142.5; 142.5; 142.5; 142.5. 300; 143.0; 143.0; 143.0; 143.0; 143.5. 310; 143.5; 143.5; 144.0; 144.0; 144.0. 320; 144.0; 144.5; 144.5; 144.5; 144.5. 330; 144.5; 145.0; 145.0; 145.0; 145.0. 340; 145.0; 145.5; 145.5; 145.5; 145.5. 350; 146.0; 146.0; 146.0; 146.0; 146.0. 360; 146.0; 146.0; 146.5; 146.5; 146.5. - 903.5.2.3 In-situ Density #### The density of the compacted concrete shall be such that the total air voids are not more than 3 per cent. The air voids shall be derived from the difference between the theoretical maximum dry density of the concrete calculated from the specific gravity of the constituents of the concrete mix and the average value of three direct density measurements made on cores at least 150 mm diameter. Three cores shall be taken from trial lengths and in first two km length of the pavement, while the slab is being constructed during normal working. The proportions of the mix and the vibratory effort imparted i.e. the frequency and magnitude of vibration shall be adjusted to achieve the maximum density. All cores taken for density measurement in the trial section shall also be checked for thickness. The same cores shall be made use of for determining in-situ strength. In case of doubt, additional cores may be ordered by the Engineer and taken at locations decided by him to check the density of concrete slab or the position of dowel/tie bars without any compensation being paid for the same. In calculation of the density, allowance shall be made for any steel in cores. Cores removed from the main carriageway shall be reinstated with compacted concrete with mix proportions of 1 part of Portland cement : 2 parts of fine aggregate:2 parts of 10 mm nominal size single sized coarse aggregate by weight. Before filling the fine mix, the sides shall be hacked and cleaned with water. Thereafter cement-sand slurry shall be applied to the sides just prior to filling the concrete mix. - 903.5.2.4 Thickness #### Thickness shall be controlled by taking levels as indicated in Clause 902.3. Thickness of the slab at any point checked as mentioned above shall be within a tolerance of -5 mm to + 10 mm of the specified thickness as per Drawing. Thickness deficiency more than 5 mm may be accepted and paid for at a reduced rate given in Clause 602.16.3. In no case, however, thickness deficiency shall be more than 10 mm. - 903.5.2.5 Summary of Control Tests #### Table 900-6 gives a summary of frequency of testing of pavement concrete. Table 900-6 : Frequency of Quality Control Tests for Pavement Concrete 1.; Levels, alignment and texture. i) Level tolerance; Clause 902.3. ii) Width of pavement and position of paving edges; Clause 902.2. iii) Pavement thickness; Clause 902.3 and 903.5.2.4. iv) Alignment of joints, widths, depth of dowel grooves; To be checked @ one joint per 400 m length or a day’s work. v) Surface regularity both transversely and longitudinally; Once a day or one day’s work without disturbing the curing. vi) Alignment of dowel bars and their accuracy/tie bars; To be checked in trial length as per Clause 602.6.5.2 and once on every 2 km.. vii) Texture depth; Clause 602.12. 2.; Quality of materials and concrete shall be as under :. 1. Cement Physical and chemical Tests; IS:269 IS:455 IS:1489 IS:8112 IS:12269; Once for each source of supply and occasionally when called for in case of long/improper storage. Besides, the Contractor also will submit daily test data on cement released by the manufacturer. 2.Coarse and Fine Aggregates; (i) Gradation; IS:2386; One test for every day’s work of each fraction of coarse aggregate and fine aggregate, initially; (may be relaxed later at the discretion of the Engineer). (ii) Deleterious constituents; IS:2386 (Pt. 2); -do-. (iii) Water absorption; IS:2386 (Pt. 3); Regularly as required subject to a minimum of one test a day for coarse aggregate and two tests a day for fine aggregate. This data shall be used for correcting the water demand of the mix on a daily basis.. 3. Coarse Aggregate; (i) Los Angeles Abrasion value or Aggregate Impact test; IS:2386 (Pt. 4); Once for each source of supply and subsequently on monthly basis.. (ii) Soundness; IS:2386 (Pt. 5); Before approving the aggregates and every month subsequently.. (iii) Alkali aggregate reactivity; IS:2386 (Pt. 7) IS:456; -do-. 4. Water; Chemical Tests; IS:2386; Once for approval of source of supply, subsequently only in case of doubt.. 5. Concrete; (i) Strength of concrete; IS:516; 2 cubes and 2 beams per 150 cu m or part thereof (one for 7 day and other for 28 day strength) or minimum 6 cubes and 6 beams per day’s work whichever is more.. (ii) Core strength on hardened concrete; IS:516; As per the requirement of the Engineer, only in case of doubt.. (iii) Workability of fresh concrete-Slump Test; IS:1199; One test per each dumper load at both Batching plant site and paving site initially when work starts. Subsequently sampling may be done from alternate dumper.. (iv) Thickness determination; From the level data of concrete pavement surface and sub-base at grid points of 5/6.25 m x 3.5 m. (v) Thickness measurement for trial length; 3 cores per trial length. (vi) Verification of level of string line in the case of slip form paving and steel forms in the case of fixed form paving; String line or steel forms shall be checked for level at an interval of 5.0 m or 6.25 m. The level tolerance allowed shall be ± 2 mm. These shall be got approved 1-2 hours before the commencement of the concreting activity.. ---------------------- | - GENERAL - All materials to be used, all methods to be adopted and all works to be executed shall be strictly in accordance with the requirements of these Specifications. The Contractor will prepare the Quality Assurance Plan (QAP), Methodology and Works Programme duly considering terrain, land use, climatic conditions, etc. and get the same approved from the Engineer in the first instance. The QAP shall be substantially prepared in accordance with IRC: SP: 112. The Contractor shall set up field laboratory at location(s) approved by the Engineer and equip the same with adequate and eligible equipment and personnel in order to carry out required tests as per Specifications and/or as directed by the Engineer. The equipment and other provisions of the laboratory and upkeep & maintenance thereof shall be as per Clause 124 and/or as directed by the Engineer. The list of equipment and the provisions of the field laboratory shall be prepared by Contractor as part of QAP and get the same approved from the Engineer in advance before execution of Works. The equipment shall be duly calibrated as per manufacturer’s guidelines and IRC: SP: 112. The Contractor’s laboratory shall be manned by a qualified Material Engineer assisted by suitable number of Quality Control/Assistant Quality Control Engineer and experienced lab technicians, and the personnel list shall be got approved by the Engineer. The Contractor shall carry out quality control tests on the materials, processes and works to the frequency stipulated in subsequent paragraphs. In the absence of clear indications about method and or frequency of tests for any item, the instructions of the Engineer shall be followed. For carrying out tests, unbiased sample shall be collected using random sampling techniques which shall be outlined in the QAP. All the tests shall be witnessed by the personnel of the Engineer. In respect of factory manufactured materials, products and finished items for which testing facility is not available at Contractor’s field laboratory, Contractor shall furnish all the documents required vide IRC: SP: 112 to Engineer and Engineer shall duly verify the same. Any clarification sought by Engineer shall be obtained by the Contractor from the manufacturer and submit to Engineer for his satisfaction. In addition, Engineer shall witness certain tests in the laboratory of the manufacturer as specified in Contract Agreement or relevant IRC standards/guidelines/code of practice/manual and may also cause certain test(s) to be carried out in specific third-party laboratory. - For satisfying about the quality of the materials, processes and works, certain quality control tests will also be conducted by the Engineer by its own quality control unit or any other laboratory deemed fit by the Engineer and to the frequency as decided by the Engineer or as specified in Contract Agreement. - The Contractor shall provide necessary co-operation and assistance in obtaining the samples for tests and carrying out the field tests as required by the Engineer from time to time. This shall include provision of laboratory equipment, transportation, consumables, personnel including labour attendants, assistants in packing and dispatching and any other assistance considered necessary in connection with the tests. - For the work of embankment, subgrade and pavement courses, construction of subsequent layer of same or other material over the finished layer shall be done after obtaining permission from the Engineer. Similar permission from the Engineer shall also be obtained in respect of all other item of Works prior to proceeding with the next stage of construction. - The Contractor shall carry out modifications in the procedure of Works, if found necessary or as directed by the Engineer. Works falling short of quality shall be rectified/ redone by the Contractor at his own cost, and defective work shall also be removed from the site of Works by the Contractor at own cost. - The cost of laboratory building including essential supplies like water, electricity, sanitary services and their maintenance and cost of all equipment, tools, materials, labour and incidentals to perform tests and other operations of quality assurance and quality control according to the Specifications requirements shall be deemed to be incidental to the work and no payment shall be made for the same. If, however, there is a separate item in the Bill of Quantities for setting up of a laboratory and installing testing equipment, such work shall be paid for separately. - For testing of soil/soil mixes, granular materials and mixes, bituminous materials and mixes, cement concrete materials and mixes, aggregates, cores extracted from concrete and pavement courses, etc., samples in the required quantity and form shall be supplied by the Contractor at his own cost. - For cement, bitumen, steel, emulsion, road marking paint, sign boards, geo-synthetics and similar other factory manufactured materials, products and specialized items where essential tests are carried out in the presence of Engineer at the manufacturer’s plants or at laboratories other than the site laboratory, the cost of samples, sampling, testing and furnishing of test certificates shall be borne by the Contractor. In respect of materials and mixes where site testing facility is available at Contractor’s laboratory but there is high inconsistency of results or in the opinion of the Engineer, the test results need further validation, Engineer may order tests to be conducted in any outside laboratory and the cost of samples, sampling, testing and furnishing of test certificates shall be borne by the Contractor. - The method of sampling and testing of materials shall be in accordance with the requirements of the relevant Indian Standards and these Specifications. Where they are contradiction, the provisions in these Specifications shall be followed. Where they are silent, sound engineering practices shall be adopted. The sampling and testing procedure to be used shall be as approved by the Engineer and his decision shall be final and binding on the Contractor. The cost of all tests shall be borne by the Contractor. - The materials for embankment construction shall be got approved from the Engineer. The responsibility for arranging and obtaining the land for borrowing or exploitation in any other way shall rest with the Contractor who shall ensure smooth and uninterrupted supply of materials in the required quantity during the construction period. Similarly, the supply of aggregates and other materials for construction shall be from sources approved by the Engineer. Responsibility for arranging uninterrupted supply of materials from the source shall be that of the Contractor. - Defective Materials All materials which the Engineer has determined as not conforming to the requirements of the Specifications shall be rejected whether in place or not; those shall be removed immediately from the site as directed. Materials, which have been subsequently corrected, shall not be used in the Works unless approval is accorded in writing by the Engineer. Upon failure of the Contractor to comply with any instruction of the Engineer, the Engineer shall have authority to cause the removal of rejected materials and to deduct the removal cost thereof from any payments due to the Contractor. # Imported Materials The Contractor shall furnish a list of materials/finished products manufactured, produced or fabricated outside India which is proposed to be used in the Works. The Contractor shall not be entitled to extension of time for acts or events occurring outside India and it shall be the Contractor’s responsibility to make timely delivery to the job site of all such materials obtained from outside India. The materials imported from outside India shall conform to the relevant Specifications of the Contract. In case where materials/finished products are not covered by the Specifications in the Contract, the details of laboratories/establishments where tests are to be carried out shall be specifically brought out and agreed to in the Contract. The Contractor shall furnish to the Engineer a certificate of compliance of the tests carried out. In addition, certified mill test reports clearly identified in the lot of materials shall be furnished at the Contractor’s cost. # CONTROL OF ALIGNMENT, LEVEL AND SURFACE REGULARITY - General All Works performed shall conform to the lines, grades, cross sections and dimensions shown on the drawings or as directed by the Engineer, subject to the permitted tolerances described herein-after. # Horizontal Alignment Horizontal alignment shall be reckoned with respect to the center line of the carriageway as shown on the drawings. The edges of the carriageway as constructed shall be correct within a tolerance of ± 10 mm therefrom. The corresponding tolerance for edges of the roadway and lower layers of pavement shall be ± 25 mm. # Surface Levels The levels of the subgrade and different pavement courses as constructed, shall not vary from those calculated with reference to the longitudinal and cross-profile of the road shown on the drawings or as directed by the Engineer beyond the tolerances mentioned in Table 900-1. Table 900-1 : Tolerances in Surface Levels 1); Subgrade; ±20 mm. 2); Sub-base - Flexible pavement - Concrete pavement; ±10 mm ±6 mm. 3); Base-course for flexible pavement - Bituminous Base/Binder course - Granular/Stabilised - Machine laid - Manually laid; ±6 mm ±10 mm ±15 mm. 4); Wearing course for flexible pavement - Machine laid - Manually laid; ±6 mm ±10 mm. 5); Cement concrete pavement; ±5 mm. Provided, however, that the negative tolerance for bituminous layer(s) and PQC wearing course shall not be permitted in conjunction with the positive tolerance for underneath base course, if the thickness of the former is thereby reduced by more than the following limits: - 4 mm for bituminous layer of thickness 40 mm or more - 3 mm for bituminous layer of thickness less than 40 mm - 5 mm for concrete pavement slab For checking compliance with the above requirement for subgrade, sub-base and base course, measurements of the surface levels shall be taken on a grid of points placed at 6.25 m longitudinally and 3.5 m transversely. For any 10 consecutive measurements taken longitudinally or transversely, not more than one measurement shall be permitted to exceed the tolerance as above, this one measurement being not in excess of 5 mm above the permitted tolerance. For checking the compliance with the above requirement for bituminous layer(s) and PQC wearing course, measurements of the surface levels shall be taken on a grid of points spaced at 6.25 m along the length and at 0.5 m from the edges and at the center of the pavement. In any length of pavement, compliance shall be deemed to be met for the final road surface, only if the tolerance given above is satisfied for any point on the surface. # Surface Regularity of Pavement Courses The longitudinal profile shall be checked with a 3-metre-long straight edge/moving straight- edge as directed by the Engineer at the middle of each traffic lane along a line parallel to the center line of the road. The maximum permitted number of surface irregularities shall be as per Table 900-2. # Table 900-2 : Maximum Permitted Number of Surface Irregularities Irregularity; Surfaces of Carriageways and Paved Shoulders; Surfaces of Laybys, Service Areas and all Bituminous Base Courses. 4 mm; 7 mm; 4 mm; 7 mm. Length (m); 300; 75; 300; 75; 300; 75; 300; 75. Number of Surface Irregularities on National Highways/ Expressways*; 15; 9; 2; 1; 40; 18; 4; 2. Number of Surface Irregularities on Roads of lower Category*; 40; 18; 4; 2; 60; 27; 6; 3. *Category of each section of road as described in the Contract. The maximum allowable difference between the road surface and underside of a 3 m straight- edge when placed parallel with, or at right angles to the centre line of the road at points decided by the Engineer shall be: for pavement surface (bituminous and cement concrete); 3 mm. for bituminous base courses; 6 mm. for granular/stabilised sub-base/base courses; 8 mm. for sub-bases under concrete pavements; 10 mm. for subgrade; 15 mm. # 902.5 Rectification Where the surface regularity of subgrade and the various pavement courses fall outside the specified tolerances in Clause 902.4, the Contractor shall be liable to rectify these in the manner described below and to the satisfaction of the Engineer. - Subgrade: Where the surface is high, it shall be trimmed and suitably compacted. Where the same is low, the deficiency shall be corrected by scarifying the lower layer and adding fresh material and recompacting to the required density. The degree of compaction and the type of material to be used shall conform to the requirements of Clause 305 - Granular Sub-base: Same as at (i) above, except that the degree of compaction and the type of material to be used shall conform to the requirements of Clause 401. - Sub-base/base: For stabilised materials where the surface is high, the same shall be suitably trimmed while taking care that the material below is not disturbed due to this operation. However, where the surface is low, the same shall be corrected as described herein below: When the time elapsed between detection of irregularity and the time of mixing of the material is less than 2 hours, the surface shall be scarified to a depth of 50 mm, supplemented with freshly mixed materials as necessary and recompacted as per the relevant specification. When this time is more than 2 hours, the full depth of the layer shall be removed from the pavement and replaced with fresh material to Specification. This shall also apply to lime treated material except that the time criterion shall be 3 hours instead of 2 hours. - Bituminous Constructions: For bituminous construction other than wearing course, where the surface is low, the deficiency shall be corrected by adding fresh material over a suitable tack coat, if needed, and recompacting as per specifications. Where the surface is high, the extra thickness in the affected layer shall be removed and the layer recompacted to Specifications. For wearing course, where the surface is high or low, the full depth of the layer shall be removed and replaced with fresh material and compacted to specifications. In all cases where the removal and replacement of a bituminous layer is involved, the area treated shall not be less than 5 m in length and not less than 3.5 m in width. - Dry Lean Concrete Sub-Base: The defective length of the course shall be removed to full depth and replaced with material conforming to Clause 601. The area treated shall be at least 3 m long, not less than 1-lane width and extend to the full depth. Before relaying the course, the disturbed subgrade or layer below shall be corrected by levelling, watering and compacting. - Cement Concrete Pavement: The defective areas having irregularity exceeding 3 mm but not greater than 6 mm when tested with a 3-metre-long straight edge may be rectified by scrabbling or grinding using approved equipment. When required by the Engineer, areas which have been reduced in level by the above operation(s) shall be retextured in an approved manner either by cutting grooves (5 mm deep) or roughening the surface by hacking the surface. If high areas in excess 6 mm or low areas in excess of 3 mm occur, exceeding the permitted numbers and if the Contractor cannot rectify, the slab shall be demolished and reconstructed at the Contractor’s expense and in no case the area removed shall be less than the full width of the lane in which the irregularity occurs and full length of the slab. If deemed necessary by the Engineer, any section of the slab which deviates from the specified levels and tolerances shall be demolished and reconstructed at the Contractor’s cost. # 902.6 Riding Quality The measured roughness of newly constructed flexible pavement and rigid pavement before opened to traffic shall not be more than 2000 mm/km and 2200mm/km respectively. # QUALITY CONTROL TESTS DURING CONSTRUCTION - General The materials supplied and the Works carried out by the Contractor shall conform to the Specifications prescribed in the Clauses for the relevant items of Works. For ensuring the requisite quality of construction, the materials and Works shall be subjected to quality control tests, as described hereinafter. The testing frequencies set forth are the desirable minimum and the Engineer shall have the full authority to carry out additional tests as frequently as he may deem necessary, to satisfy himself that the materials and Works comply with the appropriate Specifications. However, the number of tests recommended in Tables 900-3 and 900-4 may be reduced at the discretion of the Engineer if it is felt that consistency in the quality of materials can still be maintained with the reduced number of tests. Test procedures for the various quality control tests are indicated in the respective Sections of these Specifications or for certain tests within this Section. Where no specific testing procedure is mentioned, the tests shall be carried out as per the prevalent accepted engineering practices to the directions of the Engineer. Table 900-3 : Quality Control Tests for Sub-Bases and Bases (Excluding Bitumen Bound Bases) Sl.; Pavement Course; Test; Frequency (min.). 1.; Granular Subbase; i) Gradation; One test per 800 cu m subjected to min one test per day of production.. ii) Atterberg limits; -do-. iii) Moisture content prior to compaction; One test per 400 cu m. iv) Density of compacted layer; One set of 5 measurements per 5000 sq m. v) Deleterious constituents/ Soundness; As required. vi) Water Absorption/AIV/MDD- OMC/CBR; One test on fortnightly basis.. 2.; Lime/Cement Stabilised Soil Sub-base; i) Quality of lime/ cement; One test for each consignment subject to a minimum of one test per 5 tonnes. ii) Lime/Cement content; Regularly, through procedural checks. iii) Degree of pulverization; Periodically as considered necessary. iv) CBR or Unconfined Compressive Strength test on a set of 3 specimens; 5 tests per 800 cu m subject to minimum five tests per day of production. v) Moisture content prior to compaction; One set of two tests per 500 sq m. vi) Density of compacted layer; One set of 5 measurements per 1250 sq m. vii) Deleterious constituents; As required. 3.; Wet Mix Macadam; i) Aggregate Impact Value/Water Absorption/MDD-OMC/CBR; One test on fortnightly basis.. ii) Grading of aggregate; One test per 500 cu m subjected to min one test per day of production. iii) Combined Flakiness and Elongation Indices; -do-. iv) Atterberg limits of portion of aggregate passing 425-micron sieve; -do-. v) Density of compacted layer; One set of 5 measurements per 1500 sq m. vi) Deleterious constituents/Soundness; As required. 5.; Cement Treated Subbase (CTSB); i) Gradation; One test per 800 cu m subjected to min one test per day of production.. ii) Atterberg limits; -do-. iii) Moisture content prior to compaction; One test per 400 cu m. iv) Density of compacted layer; One set of 5 measurements per 5000 sq m. v) Deleterious constituents/Soundness; As required. vi) Water Absorption/AIV/MDD- OMC; One test on fortnightly basis.. vii) Cement Content (BS:1924: Part 2 or ASTM D 806); One test per 800 cu m subjected to min one test per day of production.. viii) Unconfined Compressive Strength; Five tests per 800 cu m subject to min five tests per day of production. ix) Quality of Cement; One test for each consignment subject to a minimum of one test per 5 tonnes. x) Time of loading at plant and final compaction at site.; For each truck load.. 6.; Cement Treated Base (CTB); i) Aggregate Impact Value/ Water Absorption/ MDD-OMC; One test on fortnightly basis.. ii) Grading of aggregate; One test per 500 cu m subjected to min one test per day of production. iii) Combined Flakiness and Elongation Indices; -do-. iv) Atterberg limits of portion of aggregate passing 425 micron sieve; -do-. v) Density of compacted layer; One set of 5 measurements per 1500 sq m. vi) Deleterious constituents/Soundness; As required. vii) Cement Content (BS:1924: Part 2 or ASTM D 806); One test per 500 cu m subjected to min one test per day of production.. viii) Unconfined Compressive Strength; Five tests per 500 cu m subject to min five tests per day of production. ix) Quality of Cement; One test for each consignment subject to a minimum of one test per 5 tonnes. x) Time of loading at plant and final compaction at site.; For each truck load.. xi) Flexural Strength; One test on fortnightly basis. xii)Durability Test as per BS:4332:Part IV; One test on monthly basis. xiii) Unconfined Compressive Strength of Field Core; One Core per day of CTB laying. Table 900-4 : Quality Control Tests for Bituminous Works Sl.No.; Pavement Course; Test; Frequency (min.). 1.; Prime Coat/ Tack Coat/ Fog Spray; - Quality of binder - Binder temperature for application - Rate of spread of Binder; Number of samples per lot and tests as per IS:73, IS:217 and IS:8887 as applicable At regular close intervals Three tests per day of spray. 2.; Seal Coat/ Surface Dressing/ Crack Prevention Course SAM/ SAMI; - Quality of Binder; Same as mentioned under Serial No. 1. - Aggregate Impact Value or Los Angeles Abrasion Value - Combined Flakiness and Elongation Indices; One test per 200 cu m of aggregates each source and whenever there is change in the quality of aggregate One test per 100 cu m of aggregates for each source and whenever there is change in the quality of aggregates. (iv) Stripping value of aggregates (Immersion Tray Test); One test of each source of aggregates and whenever there is change in the quality of aggregates. - Water absorption of aggregate - Water sensitivity of mix - Grading of aggregate - Soundness (Magnesium Sulphate/ Sodium Sulphate); -do- -do- Two tests per day of laying One test for each source of aggregates and whenever there is change in the quality of aggregates. (ix) Polished stone value (not applicable for SAM/SAMI); -do-. - Temperature of binder in boiler, aggregate in dryer and mix at the time of laying and compaction - Rate of spread of binder/aggregates as applicable - Percentage of fractured faces (When gravel is used) - Geosynthetics; At regular intervals as directed by the Engineer. As regular close intervals. One test per 100 cu m of aggregates. The requirements of Section 700 shall apply. 3.; Dense Bituminous Macadam/Bituminous Concrete/ Warm Mix Asphalt/ Recycled Asphalt Pavement/ Open Graded Friction Course with and without using other additives viz waste plastic/ crumb rubber/cellulose fibre/ rejuvenator; - Quality of binder; Number of samples per lot and tests as per IS:73 or IRC:SP:53, IS:15462/ IS 17079 and other respective IRC Code as applicable One test per 350 cu m of aggregates for each source and whenever there is change in the quality of aggregates One test per 350 cu m of aggregates for each source and whenever there is change in the quality of aggregates One test for each source of aggregates and whenever there is change in the quality of aggregates. (ii) Aggregate Impact Value/ Los Angeles Abrasion Value. (iii) Flakiness and Elongation Indices. (iv) Soundness test (Sodium or Magnesium Sulphate). (v) Water absorption of aggregates; One test for each source of aggregates and whenever there is change in the quality of aggregates. (vi) Sand equivalent test; One test for each source of aggregates and whenever there is change in the quality of aggregates. (vii) Plasticity Index; One test for each source of aggregates and whenever there is change in the quality of aggregates. (viii) Polished stone value; One test for each source of aggregates and whenever there is change in the quality of aggregates. - Percentage of fractured face (when crushed gravel is used) - Mix grading - Stability and voids analysis of mix including theoretical maximum specific gravity of loose mix; One test per 350 cu m of aggregates One set for individual constituent and mixed aggregates from dryer for each 400 tonnes of mix subject to minimum of two tests per day of production per plant Three tests for stability, flow value, density and void contents for each 400 tonnes of mix subject to minimum of two tests per day of production per plant. (xii) Moisture Susceptibility of mix (AASHTO T283); One test for each mix type whenever there is change in the quality or source of coarse or fine aggregates. - Temperature of binder in boiler, aggregate in dryer and mix at the time of laying and compaction - Binder content - Rate of spread of mix material - Density of Compacted layer - Resilient modulus estimated from indirect tensile strength test on specimens prepared using field mix; At regular intervals as directed by the Engineer One set for each 400 tonnes of mix subject to minimum of two tests per day of production per plant After every 5th truck load One set of 10 measurements per 5005 sq m area Three specimens for each 400 tonnes of mix subject to minimum 2 tests per day of laying. 4.; Sand Asphalt Base course; - Quality of binder - Aggregate Impact Value or Los Angeles Abrasion Value - Sand equivalent test - Plasticity Index - Mix grading & binder content - Stability of Mix; Same as mentioned under Serial No. 2 Same as mentioned under Serial No. 2 Same as mentioned under Serial No. 2 Same as mentioned under Serial No. 5 Same as mentioned under Serial Nos. 2 and 3 Same as mentioned under Serial No. 5. - Control of temperature of binder in boiler, aggregate in the dryer and mix at the time of laying and rolling - Thickness of layer - Density of Compacted layer; Same as mentioned under Serial No. 2 Same as mentioned under Serial No. 5 Same as mentioned under Serial No. 5. 5.; Slurry Seal and Micro surfacing; - Quality of Aggregate Sand Equivalent Value Water Absorption Soundness Test (Sodium/ Magnesium Sulphate Test) - Quality of Emulsion - Aggregate Moisture - Aggregate Gradation - Binder Content - Calibration of Machine - Quantity of Slurry (By weight of aggregate); One test per source/ site One test per lot of 20 t as per IS:8887 Two test per day Two test per day at site Two test per lane per km Once per project or as and when required Daily (Travel time of Machine). 6.; Stone Matrix Asphalt; - Quality of binder - Aggregate Impact Value/ Los Angeles Abrasion Value - Flakiness and Elongation Indices; Number of samples per lot and tests as per IS:15462 One test per 100 cu m of aggregates One test per 100 cu m of aggregates. - Soundness Test (Sodium and Magnesium Sulphate Test) - Water absorption of aggregate - Sand equivalent test - Plasticity Index - Polished stone value - Percent of fractured faces (when crushed gravel is used); One test for each method for each source of aggregates and whenever there is change in the quality of aggregates One test for each source of aggregates and whenever there is change in the quality of aggregates One test for each source of aggregates One test for each source of aggregates One test for each source of aggregates One test per 50 cu m of aggregates. - Mix grading - Air voids and VMA analysis of mix including theoretical maximum specific gravity of loose mix - Moisture Susceptibility of mix (AASHTO T 283) - Temperature of binder in boiler, aggregate in dryer and mix at the time of laying and compaction; One set for individual constituent and mixed aggregates from dryer for each 400 tonnes of mix subject to minimum of two tests per day of production per plant Three tests per day of production One test for each mix type whenever there is change in the quality or source of coarse or fine aggregates At regular intervals as directed by the Engineer. (xiv) Binder content; One set for each 400 tonnes of mix subject to minimum of two tests per day of production per plant. (xv) Rate of spread of mix material; After every 5th truck load. - Density of compacted layer - Binder Drain Down; One set of 10 measurements per 2500 sq m area One test at start of the production for the day. 7.; Mastic asphalt; - Quality of binder - Aggregate Impact Value and Los Angeles Abrasion Value - Combined Flakiness and Elongation Indices - Stripping value - Water Sensitivity of mix; Same as mentioned under Serial No 3 Same as mentioned under Serial No. 3 Same as mentioned under Serial No. 3 Same as mentioned under Serial No. 2 Same as mentioned under Serial No. 3. - Grading of aggregates - Water absorption of aggregates - Soundness (Magnesium Sulphate/ Sodium Sulphate) - Percentage of fractured faces - Binder content and aggregate grading; Two tests per day of production per plant on the individual constituents and mixed aggregates from the dryer Same as mentioned under Serial No. 3 Same as mentioned under Serial No. 3 Same as mentioned under Serial No. 3 Same as mentioned under Serial No. 3. - Control of temperature of binder and aggregate for mixing and of the mix at the time of laying and rolling - Rate of Spread of Mixed Material - Hardness number; At regular intervals as directed by the Engineer Regular control through check of layer thickness Minimum two tests per day of laying. 8.; Cold Mixes (Emulsion/Foamed Bitumen Stabilised Material); i)-; All test & its frequency Same as Sr. No. 5.. ii) ITS dry & ITS wet; One set of testing comprised of 3- specimens each for Dry & wet conditions for each 500 ton of mix.. iii) MDD/OMC; One test on fortnightly basis.. Note: Daily, weekly, monthly reports on test results shall be prepared indicating the location of sampling and testing, deviation from the specified values for materials and Works and remedial action taken in respect of removal of defective Works shall be prepared by the Contractor. The test record shall be duly certified by the Engineer that these tests were done in his presence and testing carried out as per prescribed methodology. # Tests on Earthwork For Embankment, Subgrade Construction and Cut Formation - Borrow Material Grid the borrow area at 25 m c/c (or closer, if the variability is high) to full depth of proposed working. These pits should be logged and plotted for proper identification of suitable sources of material. The following tests on representative samples shall be carried out for every 3000 cum for each source: - Sand Content [IS:2720 (Part-4)]: 2 tests per 3000 cu m of soil. - Plasticity Test [IS:2720 (Part-5)]: Each soil type to be tested, 2 tests. - Density Test [IS:2720 (Part-8)]: Each soil type to be tested, 2 tests. - Deleterious Content Test [IS:2720 (Part-27)]: As and when required by the Engineer. - Moisture Content Test [IS:2720 (Part-2)]: Two tests. - CBR Test on materials to be incorporated in the subgrade on soaked samples [IS:2720 (Part-16)]: One CBR test (average of three specimens) or closer as and when required by the Engineer. - Free Swelling Index (FSI) [IS: 2720 (Part-40)]: Two tests. # Compaction Control Control shall be exercised on each layer by taking at least one set of ten measurements of density for each 3000 sq m of compacted area, or closer as required to yield the minimum number tests results for evaluating a day’s work on statistical basis. The determination of density shall be in accordance with IS: 2720 (Part-28). Test locations shall be chosen only through random sampling techniques. If non-destructive tests are carried out, the number of tests shall be doubled. If considerable variations are observed between individual density results, the minimum number of tests in one set of measurement shall be increased. The acceptance criteria shall be subject to the condition that the mean density is not less than the specified density plus: However, for earthwork/granular material in unpaved shoulders and in the subgrade, at least one set of ten density measurements shall be taken for every 2000 sq. m for the compacted area. In other respects, the control shall be similar to that described earlier. # Cut Formation Tests for the density requirements of cut formation shall be carried out in accordance with Clause 903.2.2. # Tests on Sub-Bases and Bases (Excluding Bitumen Bound Bases) The tests and their frequencies for the different types of bases and sub-bases shall be given in Table 900-3. The evaluation of density results and acceptance criteria for compaction control shall be on lines similar to those set out in Clause 903.2.2 except that test area for one set of measurements and number of measurements for 1 set shall be as specified in Table 900-3. - Acceptance Criteria for tests on the strength of cement/ lime stabilized subbase, CTSB & CTB (CBR/UCS) Control shall be excercised by taking at least one set of 5 test for each 800 cu m subjected to minimum 5 test for each day production. The acceptance criteria for tests on the strength of cement/lime stabilized soil and distribution of stabilizer content shall be subject to the condition that the mean value is not less than the specified value plus: # Tests on Bituminous Construction 903.4.1 Tests and Frequency The tests for the different types of bituminous works shall be as given in Table 900-4. The Engineer may direct additional testing as required. # Acceptance Criteria The acceptance criteria for tests on density shall be subject to the condition that the mean value is not less than the specified value plus: - Quality Control Tests for Concrete Road Construction - Dry Lean Concrete Sub-base - Sampling for Cube Specimens Samples of dry lean concrete for making cubes shall be taken from the uncompacted material from different locations using random sampling techniques immediately before compaction at the rate of 3 samples for each 1000 sq m or part thereof laid each day. Test cubes of 150 mm size shall be prepared immediately from each mix sample. Cubes shall be made in accordance with the methods described in IS:516 except that the cubes shall be compacted by means of a vibratory hammer with the moulds placed on a level and rigid base. The vibrating hammer shall be electric or pneumatic type fitted with a square or rectangular foot having an area between 7500 to 14000 sq.mm. The compaction shall be uniformly applied for 60± 5 seconds with a downward force between 300 N and 400 N on to each of the three layers of the lean concrete material placed into the mould. The surface of each compacted layer shall be scarified before the next layer is added to give key for the next layer. The final layer shall be finished flush with the top of the cube mould. The dry lean concrete shall be cured in accordance with IRC: SP: 49/IS: 516. - In-situ Density The dry density of the laid material shall be determined from three density tests at locations equally spaced along a diagonal that bisects each 2000 sq m or part thereof laid each day and shall comply with the requirements as per Clause 601.6.5.1. This rate of testing may be increased at the discretion of the Engineer in case of doubt or to determine the extent of defective area in the event of non-compliance. Density tests may be made at random to check the density at edges. 903.5.1.3 Thickness The average thickness of the DLC subbase layer as computed by the level data of sub-base and subgrade or lower sub-base shall be as per the thickness specified in the contract drawings. The thickness at any single location shall not be 8 mm less than the specified thickness. Such areas shall be corrected as stated in Clause 601.6.5.5. Areas which cannot be repaired should be replaced over full width. The extent of deficient area should be decided based on cores. # Frequency of Quality Control Tests The quality control tests for levels, alignment, materials and concrete mix shall be as given in Table 900-5. - Pavement Quality Concrete - Sampling, Testing and Acceptance Criteria for Beam and Cube Specimens Six number each of cubes & beams specimens shall be cast for every 150 cu m (or part thereof) of concrete placed during construction. Out of total cubes and beams specimens cast for each day of production, half of the same shall be tested for 7-days strength and remaining shall be tested for 28-days strength. On each day’s work, not less than six numbers each of cubes and beams specimens shall be made for each type of mix from the concrete delivered to the paving plant. Each pair of beam and cube shall be from a different delivery of concrete and tested at a place to be designated by the Engineer in accordance with the testing procedure as outlined in Clause 602.3.3. The specimens shall be transported in an approved manner to prevent sudden impact causing fractures or damage to the specimen. The flexural strength test results shall prevail over compressive strength test for compliance. 903.5.2.2 A quality control chart indicating the strength values of individual specimens shall be maintained for continuous quality assurance. Where the requirements are not met with, or where the quality of the concrete or its compaction is suspect, the actual strength of the concrete in the slab shall be ascertained by carrying out tests on cores cut at the rate of 2 cores for every 150 cu m. of concrete. The average of the results of crushing strength tests on these cores shall not be less than 0.8 x 0.85 times the corresponding characteristic compressive strength of cubes, where the height to diameter ratio of the cores is two. Where height to diameter ratio is not two, necessary corrections shall be made in calculating the crushing strength of cubes in the following manner.: The crushing strengths of cylinders with height to diameter ratios between 1 and 2 may be corrected to correspond to a standard cylinder of height to diameter ratio of 2 by multiplying with the correction factor obtained from the following equation: f = 0.11 n+0.78 where f = correction factor and n = height to diameter ratio The corrected test results shall be analysed for conformity with the specification requirements for cube samples. Where the core tests are satisfactory, they shall have precedence for assessing concrete quality over the results of moulded specimens. The diameter of cores shall not be less than 150 mm. If, however, the tests on cores also confirm that the concrete is not satisfying the strength requirements, then the concrete corresponding to the area from which the cores were cut should be replaced, i.e., at least over an area extending between two transverse joints where the defects could be isolated or over larger area, if necessary, as assessed by additional cores and their test results. The equivalent flexural strength at 28 days shall be estimated in accordance with Clause 602.3.3.2. In order to ensure that the specified minimum strength at 28 days is attained in 1 in 20 of all test beams, the mix shall be proportioned to give an average strength at 28 days exceeding the specified strength by 1.65 times the standard deviation calculated first from the flexural strength of test beams made from the trial mix and subsequently from the accumulating result of flexural strengths of job control test beams. The standard deviation shall be re-calculated from the test results obtained after any change in the source or quality of materials and the mix shall be adjusted as necessary to comply with the requirements. An individual 28 day test strength below the specified strength shall not be evidence for condemnation of the concrete concerned if the average 28 day strength of this beam plus the preceding 5 and succeeding 4 beams exceeds the specified strength by 1.65 times the standard deviation and provided that there is no other evidence that the concrete mix concerned is substandard. Beams shall be made each day in pairs at intervals, each pair being from a different batch of concrete. At the start of the work, and until such time as the Engineer may order a reduction in the number of beams required, at least six pairs of beams and cubes shall be made each day, one of each pair for testing at 28 days for determination of minimum permissible flexural strength and the other for testing at an early age for the Engineer to assess the quality of the mix. When the first thirty number of 28-day results are available, and for so long as the Engineer is satisfied with the quality of the mix, he may reduce the number of beams and cubes required. During the course of construction, when the source of any material is to be changed, or if there is any variation in the quality of the materials furnished, additional tests and necessary adjustments in the mix shall be made as required to obtain the specified strength. The flexural strengths obtained from beams tested before 28 days shall be used in conjunction with a correlation between them and the 28 day flexural strengths to detect any deterioration in the quality of the concrete being produced. Any such deterioration shall be remedied without awaiting the 28 day strengths but the earlier strengths shall not constitute sole evidence of non-compliance of the concrete from which they were taken. As per IRC:15, the concrete is said to comply with the specified flexural strength, when the following conditions are met with: The mean strength determined from any group of 4 consecutive samples (each sample containing 3 beam specimen i.e. 4 x 3 = 12 beam specimens) at 28 days should exceed the specified characteristic flexural strength by at least 0.3 MPa. The strength of any sample is not less than the specified characteristic flexural strength minus 0.1 MPa. Should the concrete fail to comply with the Specifications for strength as described above, the Contractor may, all at his own expense, elect to cut cores from the suspect concrete as the Engineer shall direct. From the relation between cube strength and flexural strength, the core strength shall be converted to flexural strength. Age factors shall not to be applied on cores while determining the strength as per IRC:15. Any concrete that fails to meet the strength Specifications shall be removed and replaced at Contractor’s expense. 905.2.2.3 In-situ Density The density of the compacted concrete shall be such that the total air voids are not more than 3 per cent. The air voids shall be derived from the difference between the theoretical maximum dry density of the concrete calculated from the specific gravity of the constituents of the concrete mix and the average value of three direct density measurements made on cores at least 150 mm diameter. Three cores shall be taken from trial lengths and in first two km length of the pavement, while the slab is being constructed during normal working. The proportions of the mix and the vibratory effort imparted i.e. the frequency and magnitude of vibration shall be adjusted to achieve the maximum density. All cores taken for density measurement in the trial section shall also be checked for thickness. The same cores shall be made use of for determining in-situ strength. In case of doubt, additional cores may be ordered by the Engineer and taken at locations decided by him to check the density of concrete slab or the position of dowel/tie bars without any compensation being paid for the same. In calculation of the density, allowance shall be made for any steel in cores. Cores removed from the main carriageway shall be reinstated with compacted concrete with mix proportions of 1 part of Portland cement : 2 parts of fine aggregate:2 parts of 10 mm nominal size single sized coarse aggregate by weight. Before filling the fine mix, the sides shall be hacked and cleaned with water. Thereafter cement-sand slurry shall be applied to the sides just prior to filling the concrete mix. # Thickness Thickness shall be controlled by taking levels as indicated in Clause 902.3. Thickness of the slab at any point checked as mentioned above shall be within a tolerance of -5 mm to + 10 mm of the specified thickness as per Drawing. Thickness deficiency more than 5 mm may be accepted and paid for at a reduced rate given in Clause 602.16.3. In no case, however, thickness deficiency shall be more than 10 mm. # Summary of Control Tests The quality control tests for levels, alignment, materials and concrete mix shall be as given in Table 900-5. \ Table 900-5: Quality Control Tests for Dry Lean Concrete* and Pavement Quality Concrete 1.; Levels, alignment and texture. i) Level tolerance; Same as mentioned in Clause 902.3. ii) Width of pavement and position of paving edges; Same as mentioned in Clause 902.2. iii) Pavement thickness; Same as mentioned in Clause 902.3 and 903.5.2.4. iv) Alignment of joints, widths, depth of dowel grooves; To be checked @ one joint per 400 m length or a day’s work. v) Surface regularity both transversely and longitudinally; Once a day or one day’s work without disturbing the curing. vi) Alignment of dowel bars and their accuracy/tie bars; To be checked in trial length as per Clause 602.6.5.2 and once on every 2 km.. vii) Texture depth; As per Clause 602.12. 2.; Materials and Concrete. 1. Cement (Physical and chemical Tests); IS:269 IS:455 IS:1489; Once for each source of supply and occasionally when called for in case of long/improper storage. Besides, the Contractor also will submit daily test data on cement released by the manufacturer. 2. Coarse and Fine Aggregate s; (i) Gradation; IS:2386; One test for every day’s work of each fraction of coarse aggregate and fine aggregate, initially; (may be relaxed later at the discretion of the Engineer). (ii)Deleterious constituents; IS:2386 (Pt. 2); -do-. (iii) Water absorption; IS:2386 (Pt. 3); Regularly as required subject to a minimum of one test a day for coarse aggregate and two tests a day for fine aggregate. This data shall be used for correcting the water demand of the mix on a daily basis.. 3. Coarse Aggregate; (i) Los Angeles Abrasion value or Aggregate Impact test; IS:2386 (Pt. 4); Once for each source of supply and subsequently on monthly basis.. (ii) Soundness; IS:2386 (Pt. 5); Before approving the aggregates and every month subsequently.. (iii) Alkali aggregate reactivity; IS:2386 (Pt. 7) IS:456; -do-. 4. Water; Chemical Tests; IS:2386; Once for approval of source of supply, subsequently only in case of doubt.. 5. Concrete; (i) Strength of concrete; IS:516; 6 cubes and 6 beams per 150 cu m or part thereof (3 beam and 3 cube for 7 day and other for 28 day’s strength) or minimum 6 cubes and 6 beams per day’s work whichever is more.. (ii)Core strength on hardened concrete; IS:516; As per the requirement of the Engineer, only in case of doubt.. (iii) Workability of fresh concrete-Slump Test; IS:1199; One test per each dumper load at both batching plant site and paving site initially when work starts. Subsequently sampling may be done from alternate dumper.. (iv)Thickness determination; From the level data of concrete pavement surface and sub-base at grid points of 5/6.25 m x 3.5 m. (v)Thickness measurement for trial length; 3 cores per trial length. (vi) Verification of level of string line in the case of slip form paving and steel forms in the case of fixed form paving; String line or steel forms shall be checked for level at an interval of 5.0 m or 6.25 m. The level tolerance allowed shall be ± 2 mm. These shall be got approved 1-2 hours before the commencement of the concreting activity.. (vii) Flexural strength on beams extracted from hardened concrete; IS:516; As per the requirement of the Engineer, only in case of doubt.0. *Whichever is applicable for DLC. |  |